

	通信用室内双芯2.0紧套光缆
Indoor dual-core 2.0 tight-sleeve optical cable for communication


	Cable Construction Parameter 光缆结构参数

	紧套光纤芯数
Tighten the number of fiber cores
	2F

	紧套光纤颜色               Tight fiber color
	G652D

	
	白+黄

	紧套光纤材料            Tight sleeve fiber material
	PVC

	紧套光纤外径(-0.05mm)     Tight sleeve fiber outer diameter
	 Ø0.9

	紧套光纤一次剥离度(±0.5Cm) Tight sleeve fiber one-time peeling degree
	1.5cm

	紧套光纤外径不圆度        The outer diameter of the tight sleeve fiber is not round
	[bookmark: _GoBack]≤2%

	紧套光缆外径（±0.05mm）      Tight sleeve optical cable outer diameter
	1.85*3.8

	紧套光缆壁厚（±0.05mm）    Tight sleeve cable wall thickness
	0.5

	紧套光缆外护材料          Tight sleeve of optical cable outer shield material
	PVC

	紧套光缆外护颜色         Tight sleeve optical cable outer cover color
	黄色

	芳纶型号及填充数       Aramid model and filling number
	1100D*3股*2C

	抗拉（N）                         Tensile resistance
	短期
	长期

	
	320
	200

	最小弯曲半径（mm）       Minimum bending radius
	动态20D
	静态10D
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	Optical Fiber Parameter 光纤参数

	光纤品牌 
Fiber optic brand
	长飞

	光纤类型
 Fiber type
	G652D

	芯径 
Core diameter
	9μm

	芯不圆度
Core incompleteness
	≤5%

	包层直径 
Cladding diameter
	124.8 ± 1μm

	包层不圆度
 Cladding is not round
	≤ 1%

	涂层直径
 Coating diameter
	245 ± 7μm

	涂层/包层同心度误差 Coating/cladding concentricity error
	≤12um

	涂层不圆度
 The coating is not round
	≤6%

	芯/包层同心度误差 
Core/cladding concentricity error
	≤1um

	衰减系数 
Attenuation factor
	≤0.4dB/km at 1310nm, 
≤ 0.3dB/km at 1550nm
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