通信用室内双芯2.0紧套光缆 Indoor dual-core 2.0 tight-sleeve optical cable for communication

| Cable Construction Parameter 光缆结构参数 |  |  |
| --- | --- | --- |
| 紧套光纤芯数 Tighten the number of fiber cores | 2F |  |
| 紧套光纤颜色 Tight fiber color | G652D |  |
|  | 白+黄 |  |
| 紧套光纤材料 Tight sleeve fiber material | PVC |  |
| 紧套光纤外径(-0.05mm) Tight sleeve fiber outer diameter | Ø0.9 |  |
| 紧套光纤一次剥离度(±0.5Cm) Tight sleeve fiber one-time peeling degree | 1.5cm |  |
| 紧套光纤外径不圆度 The outer diameter of the tight sleeve fiber is not round | ≤2% |  |
| 紧套光缆外径（±0.05mm） Tight sleeve optical cable outer diameter | 1.85*3.8 |  |
| 紧套光缆壁厚（±0.05mm） Tight sleeve cable wall thickness | 0.5 |  |
| 紧套光缆外护材料 Tight sleeve of optical cable outer shield material | PVC |  |
| 紧套光缆外护颜色 Tight sleeve optical cable outer cover color | 黄色 |  |
| 芳纶型号及填充数 Aramid model and filling number | 1100D*3股*2C |  |
| 抗拉（N） Tensile resistance | 短期 | 长期 |
|  | 320 | 200 |
| 最小弯曲半径（mm） Minimum bending radius | 动态20D | 静态10D |

| Optical Fiber Parameter 光纤参数 |  |
| --- | --- |
| 光纤品牌 Fiber optic brand | 长飞 |
| 光纤类型 Fiber type | G652D |
| 芯径 Core diameter | 9μm |
| 芯不圆度 Core incompleteness | ≤5% |
| 包层直径 Cladding diameter | 124.8 ± 1μm |
| 包层不圆度 Cladding is not round | ≤ 1% |
| 涂层直径 Coating diameter | 245 ± 7μm |
| 涂层/包层同心度误差 Coating/cladding concentricity error | ≤12um |
| 涂层不圆度 The coating is not round | ≤6% |
| 芯/包层同心度误差 Core/cladding concentricity error | ≤1um |
| 衰减系数 Attenuation factor | ≤0.4dB/km at 1310nm, ≤ 0.3dB/km at 1550nm |